## Slide 1
Evaluating Sizing Effect on Recycled Continuous Carbon Fibres from Automotive Composites
Dionisis Semitekolos, R Nano NTUA
2nd Eurecomp Webinar
16/07/2024

## Slide 2
Professors (4)
Post Doctoral Researchers (14)
Researchers (11)
PhD (10)
Technicians (3)
Head:
Prof. Costas Charitidis
The "Research Unit of Advanced, Composite, Nano Materials & Nanotechnology", R-NanoLab is established since 2006;
has extensive experience in Designing, Production and Characterization of Advanced-, Composite- and Nano- Materials.
Zografou Campus, School of Chemical Engineering
Lavrion Technological & Cultural Park
Attica Region
Piraeus
Athens City Centre
R-Nano Lab Facilities

## Slide 3
Main Pillars of Activity
Synthesis & (nano) Materials Development (C-based, Polymer based etc.)
Composites & Circularity (Fibre production, Surface Treatment & Sizing, Composite fabrication & testing, Chemical/ Thermal Recycling)
Thermoplastics processing & Circularity (compounding, extrusion, upcycling)
r-nano.gr

## Slide 4
Introduction on Surface Treatment & Sizing of CFs
Electropolymerisation of CF fabrics
Development of nano-enhanced sizing solutions
Upgrade and evaluation of chemically recycled CFs
Sustainable sizing formulations

## Slide 5: I. Introduction on Surface Treatment & Sizing of CFs

## Slide 6
Introduction on Surface Treatment & Sizing of CFs
CF production line from PAN fibres
Image from:
https://www.sglcarbon.com/en/carbon-fibers-and-cfrp/

## Slide 7
When a load is applied to the composite, stress is transferred to the fibers through the matrix. A weak bond between the matrix and the fiber leads to degraded mechanical properties
Surface CF treatment
Too powerful bond  Brittle and fragile composite
Weak treatment  low durability composite
ideal adhesion
fibre - matrix
Introduction on Surface Treatment & Sizing of CFs
https://link.springer.com/article/10.1007/s11051-019-4743-7

## Slide 8
A successful surface treatment is bound to:
Increase the wettability of the fiber surface to the matrix resin by removal of the weak boundary layer, contaminant species or gas molecules adsorbed
Ensure the significant level of van der Waals interactions, which allow the matrix molecules to physically entangle with, or diffuse into, the molecular network of polymer CF coating
Promote mechanical interlocking between the fiber and the matrix, usually done by creating surface porosity into which resin molecules can penetrate
Increase the surface roughness, which will create new active sites on the fiber surface for subsequent chemical bonding with the unreacted species in the matrix resin
Attach a thin layer of 'coupling agent' that will chemically bond to both; fiber and matrix acting as a bridge
Image from:
https://www.intertronics.co.uk/2017/08/plasma-surface-treatment-for-bonding-composites/
https://doi.org/10.1016/j.matdes.2020.108633
Introduction on Surface Treatment & Sizing of CFs

## Slide 9
https://doi.org/10.1016/j.pcrysgrow.2018.07.001
Introduction on Surface Treatment & Sizing of CFs

## Slide 10
Oxidation
The basic means of achieving oxidation is through gases (by air, oxygen, ozone, etc.) or solutions (by HNO3, hydrochloric acid, etc.).
Parametres:
grade of CF being oxidized
concentration of oxidative medium
treatment time and
treatment temperature
Introduction on Surface Treatment & Sizing of CFs
https://doi.org/10.1016/j.compositesb.2017.09.010
https://doi.org/10.1016/j.ijhydene.2017.09.145

## Slide 11
Electrochemical oxidation
Electrochemical oxidation is used the most often in industrial practice. The oxidation can be carried out in various electrolytes under the most diverse conditions.
Parameters:
type of electrolyte,
its pH,
the polarization potential,
the duration of the treatment and
the morphology of the surface
H2SO4 or NaOH
Oxidation may occur in acidic or basic electrolytic solutions
Galvanostatic or potentiostatic
Most commonly used NaOH, HNO3, H2SO4, H3PO4, ΚΝΟ3 and ammonium salts
Increase in the number of surface functional groups in the fibers
https://doi.org/10.3390/ma14071758
Introduction on Surface Treatment & Sizing of CFs

## Slide 12
describes an electrochemical process where monomers are polymerized in solution on the surface of an electrode or in the vicinity of it.
Carbon fiber grafting
Electropolymerisation
Chemical vapor deposition
Chemical grafting
Irradiation grafting
Graphitic structure by design
Advantages
controlling the thickness
functionality of a ‘reactive’ coating through selective processing parameters
uniform coatings
https://doi.org/10.1016/j.compositesa.2019.01.014
Introduction on Surface Treatment & Sizing of CFs

## Slide 13: II. Electropolymerisation of CF fabrics
https://doi.org/10.3390/nano11102631
https://doi.org/10.3390/polym13234092
https://doi.org/10.3390/polym15030768
https://doi.org/10.1016/j.mtcomm.2022.103854
https://doi.org/10.1016/j.compstruct.2021.114780

## Slide 14
Electropolymerisation of CF fabrics
Aqueous solution H2SO4 5%
10 scanning cycles
-3V  3V  -3V
Cycle rate
0,1V/s
2 Stage Process;
1st cyclic voltammetry,
2nd electropolymerization
Aqueous Solution
0,3M MAA
0,4M ZnCl2
10mM N, N’ methylene bis acrylamide
Voltage -0,435V
time 1h

## Slide 15
Chart: Potential (V)
a
b
d
Cyclic Voltammetry
c
Formation of stage II, C48+ HSO4− •2H2SO4 (intercalated anion per two graphene layers)
Formation of stage I, C24+ HSO4− •2H2SO4 (intercalated anion per graphene layer)
Further oxidation to partially covalent graphene oxide
Reduction of surface oxides, defect oxides and partially reduced GO
Electropolymerisation of CF fabrics

## Slide 16
Chart: Time (s)
Thickness of polymer film can be derived by Faraday’s Law, taking advantage of the area below the graph that equals to the electric charge that passes through the CF
Electropolymerization
Electropolymerisation of CF fabrics

## Slide 17
Introduction on Surface Treatment & Sizing of CFs
Scanning Electron Microscopy/ Atomic Force Microscopy
Pristine
b. Electrochemical
c/d. Electropolymerised
Smooth
Rigged
Roughness increase
Exfoliation
Coating

## Slide 18
SEM analysis
Untreated T700
Electropolymerised T700
Electropolymerised T700
Rigged and smooth surface
Graft Polymerisation
Surface roughness
coating
Electropolymerisation of CF fabrics

## Slide 19
Electropolymerisation of CF fabrics
X-ray spectroscopy
C-C, C-OH
C-C, C-OH, C=O
C-C, C-OH, C=O,
COOH
18.4 % O2
18.8 % O2
26.5 % O2
α. pristine:
b. electrochemical:
c. electropolymerised:

## Slide 20
Electropolymerisation of CF fabrics
Mechanical Properties
+ 16.2% electropolymerised
+ 36.2% electropolymerised
Treated fibres coated
with epoxy
Severe delamination
on Reference

## Slide 21
Electropolymerisation of CF fabrics
a, c pristine
Voids
Detached “naked” fibres
Separated interface
b,d electropolymerised
Fewer voids
Fractured fibres with epoxy on surface
Dwindled separated interfaces

## Slide 22
Electropolymerisation of CF fabrics
Fracture Analysis
Treated fibres are coated with the matrix even after failure
Severe delamination on reference sample

## Slide 23
CFs
Designed & Manufactured by R-Nano Group
PMAA@CFs
Surface treatment on CFs via electropolymerisation of MAA
Automated Take up
Electropolymerisation of CF fabrics

## Slide 24: Fabrication of a front wing for racing car with modified materials

## Slide 25: Fabrication of energy absorber for automotive with modified materials

## Slide 26: III. Development of nano-enhanced sizing solutions for carbon fibres
https://doi.org/10.3390/fib12020016
https://doi.org/10.3390/recycling9030037

## Slide 27
Development of nano-enhanced sizing solutions for carbon fibres
Goal: Develop water based nano enhanced sizing solutions to improve compatibility of carbon fibres with 3R resins and apply functionality
Challenges:
Agglomeration of nanomaterials
Stable solutions
Effective desizing
Uniform coatings
Upscaling
Motivation

## Slide 28: Pilot scale carbon fibre sizing line

## Slide 29
Development of nano-enhanced sizing solutions for carbon fibres
Temperature parametric study of sizing removal,
operation speed 0.2m/min
350oC, (b) 400oC, (c) 450oC,
(d) 500 oC, (e) 550oC, (f) 600oC

## Slide 30
Development of nano-enhanced sizing solutions for carbon fibres
Solid content concentration study of (a) 1, (b) 2.5 and (c) 5%w at 1000x magnification, and 20000x magnification

## Slide 31
Development of nano-enhanced sizing solutions for carbon fibres
Surface morphology study of
CNTs O2,
(b) CNTs N2,
(c) CNTs NH3,
(d) FLG O2,
(e) FLG N2,
(f) FLG NH3

## Slide 32: Development of nano-enhanced sizing solutions for carbon fibres

## Slide 33
Development of nano-enhanced sizing solutions for carbon fibres

## Slide 34
Development of nano-enhanced sizing solutions for carbon fibres
The enhanced performance of N2-functionalized nanoparticles can be attributed to their chemical affinity with the sizing solution.
HP206 is amine-dispersed
N2 functionalization introduces C-N bonds (XPS)
NH3 functionalization introduces C-N bonds (XPS) but less than N2 (XPS)
O2 functionalization introduces C-O bonds (XPS)
Single fibre push out test results

## Slide 35
IV. Upgrade and evaluation of chemically recycled carbon fibres

## Slide 36
Upgrade and evaluation of chemically recycled carbon fibres
Plasma assisted solvolysis
Composite specimen manufactured with Filament Winding
Continuous Carbon Fibre Reclamation
Plasma assisted solvolysis or Chemical assisted treatment
Continuous recycled Fibre winding
Chemical assisted solvolysis

## Slide 37
Upgrade and evaluation of chemically recycled carbon fibres
100% Carbon
Reference Fibre x1000
EDS analysis of reference fibre
100% Carbon
Plasma Recycled Fibre x1000
EDS analysis of plasma recycled fibre
Plasma Recycled & Sized Fibre x1000
94% Carbon
EDS analysis of plasma recycled & sized fibre
Chemically Recycled Fibre x1000
67% Carbon
EDS analysis of chemically recycled fibre
Chemically Recycled & Sized Fibre x1000
EDS analysis of chemically recycled & sized fibre
90% Carbon
Plasma Results:
No resin residues after recycling
No visual filament damage
Good surface morphology after sizing
Chemically assisted Results:
Few resin residues after recycling
No visual filament damage
Few resin spots after sizing
Reference Results:
Smooth rigged surface

## Slide 38
Upgrade and evaluation of chemically recycled carbon fibres
Reference Fibre
Plasma Recycled & Sized Fibre
Chemically Recycled & Sized Fibre
TGA Results:
CF maintain their structural integrity for both recycling cases
There is ~3% resin residue on the CF from chemically recycling process

## Slide 39: Optical Microscopy Analysis

## Slide 40
Upgrade and evaluation of chemically recycled carbon fibres
10min polishing
20min polishing

## Slide 41
Upgrade and evaluation of chemically recycled carbon fibres
ImageJ
Python
Olympus
software
Filament count 14856 ± 1294
8.7%
Filament count 23700 ± 1391
5.9%
Filament count 23725 ± 820
3.5%

## Slide 42
Upgrade and evaluation of chemically recycled carbon fibres
Filament exhibits a 10% decrease in the sized recycled fibre
Unsized fibre exhibits quite lower tensile strength (~22%), probably due to the non uniform shape of the rod
Sample code​ | Tensile strength (GPa)​ | % to ref​
Reference​ | 2.7 ± 0.3​ | N/A​
Plasma Recycled | 2.1 ± 0.3​ | -22​
Plasma Recycled & Sized | 2.4 ± 0.4​ | -11​
Chemically Recycled | 2.2 ± 0.2​ | -18​
Chemically Recycled & Sized | 2.4 ± 0.3​ | -11​
Tensile tests on yarns (ASTM D4018)

## Slide 43
Upgrade and evaluation of chemically recycled carbon fibres

## Slide 44
Upgrade and evaluation of chemically recycled carbon fibres
SEM images of produced CNTs
Homogenous sample
CNTs/CNFs with diameters from 25nm to >100nm
The produced CNTs have been characterized in terms of their morphology (SEM)

## Slide 45: V. Future work
Sustainable sizing formulations

## Slide 46
Sustainable sizing formulations
Conventional sizings for CFs typically are epoxy-based emulsions
epoxy sizing agent,
film formers,
antistatic agents
surfactants
in a solid content of 0.5-5%
“Green” alternatives*
Minimize environmental impact
Reduce carbon footprint of manufacturing process
Sustainability in composite materials industry
*Bio-based raw materials*
derivatives from lignocellulosic biomass
plant based phenolics
vegetable oils
terpenes
& replacement of organic solvents of the sizing solutions, to aquatic

## Slide 47
Dionisis Semitekolos
diosemi@chemeng.ntua.gr
R Nano NTUA